Product Description

High performance black double sided automotive foam tape, coated with an aggressive solvent acrylic adhesive system meaning this tape is particularly suited to hostile outdoor environments.

Applications

Designed for applying to body side mouldings & emblems.

Features & Benefits

Good water resistance

UV resistant

Good weather resistance

Easy to use

Technical Performance

| Description | Units | Value | Test Method |
| --- | --- | --- | --- |
| Thickness | mm | 0.80±0.10 | GB/T 7125-1999 |
| Adhesive thickness | MM | 0.95±0.15 | GB/T 7125-1999 |
| Base material | - | Foamed IXPE | - |
| Tack | # | ≥12 | GB/T 4852-2002 |
| Holding strength | Min 70°c-500g-25mm x 25mm | ≥500 | GB/T 4851-1998 |
| 180° Peel strength | N/10mm | ≥8.0 | GB/T 7753-1987 |
| Elongation | % | ≥250 | GB/T 7753-1987 |
| Temperature resistance | °c | -4 to 90 | - |

Declaration of Conformity Information

REACH SVHC Status – NO SVHC present according to candidates list of the UK 25/06/20 & EU 17/01/22

RoHS Compliance Status – Not Applicable

Storage Details

Shelf life recommended 1 year from date of despatch at the moderate temperature and humidity environment.